Ti-6Al-7Nb 

367 is a dedicated, high-strength, titanium alloy with excellent biocompatibility for surgical implants.

Used for replacement hip joints, it has been in clinical use since early 1986.

Composition

	Al
	5.5-6.5%

	Nb    
	6.5-7.5

	Ta
	<0.50%

	Fe
	<0.25%

	N2
	<0.05%

	O2
	<0.20%

	C
	<0.08%

	H2
	<0.009%

	Ti
	~ Rem


Specifications/Designations

SN 056512 Swiss National specification 

Physical Data

	 
	Typical

	Density g/cm3(lb.cu.in) 
	4.52 (0.163)

	Beta Transus °C±15°C (°F)
	1010 (1850)


Mechanical Data

	 
	Typical

	Tensile Strength MPa ksi)
	1000 (145)

	0.2% Proof StressMPa(ksi)    
	900 (130)

	Elongation on 5D %
	12

	Reduction in Area %
	35

	Elastic Modulus GPa(Msi) 
	105 (15)


Forms Available

Rod; Bar; Forgings

