## Slide 1
MEETING with ALEC MITCHELL
April 09, 2015

## Slide 2: Agenda
WBU
TiO2 - introduction in the load : before the blending ? Directly in the press?
Practices to have an homogeneous chemical composition in the final ingot : variable chemical composition of the PAM electrode (Al, O…) ? Types of variations (2 or more levels, linear evolution…)
Different qualities of the alloying elements (Ti sponges, masteralloys…) versus the alloys qualities (standard, premium…) ?
Need to briquetting of the alloying elements to compensate the chemical composition of the TiCP boxes ? Problems with the behavior of the materials without structural strength under the plasma torch?
Use of the chips from turning, milling…?
Ideal length for the chips ? Problem if too thin : Ti fire risks  hard alpha
Limit sizes of the elements in the PAM furnace ? Causes of these limits?
Need to achieve uniform compaction of the briquettes? Particularly if presence of nitrided sponges (good compaction = fragmentation of the sponges and better elimination)

## Slide 3: Agenda
PAM
Minimum residence time versus the PAM parameters to avoid hard alpha ?
Width and depth of the liquid pool in the refining hearth ?
Melt rate suitable for premium quality with our PAM?
Processing of the skull : frequency to change the skull? Criteria (melt number, contamination…) ? Method to identify the contamination (analysis, sampling…) Practices to clean the skull?
Practices to change the skull : is it possible to perform MIG welding to have handling devices on the skull?
Need to restore the cold hearth after each campaign ?
Possibility to clean the skull via a mini-melt between 2 electrodes ? Quid of the cleaning in the bottom of the electrode (= biscuit of the VAR electrode)?
Camera in the mold zone : Best position to determine the liquid level?
Requirements to chain up the campaigns (chemical composition, quality…)?
TiAl : quid of the Al evaporation for pressures < 1 atm?

## Slide 4: Agenda
Miscellaneous
Method to weld stub / electrode in the VAR furnace?
Difference between the alloy qualities (standard / Premium / Disc quality) ?
Separation of flow between standard and PQ products?